3.11 Analysis and design of doubly reinforced rectangular beam

3.11.1 Analysis of doubly reinforced beam:

The steel that is occasionally used on the compression sides of beams is called compression steel, and beams with both tensile and compressive steel are referred to as doubly reinforced beams. Compression steel is not normally required in sections designed by the strength method because use of the full compressive strength of the concrete decidedly decreases the need for such reinforcement, as compared to designs made with the working-stress design method.

Occasionally, however, space or aesthetic requirements limit beams to such small sizes that compression steel is needed in addition to tensile steel.

- To increase the moment capacity of a beam beyond that of a tensile

- reinforced beam with the maximum percentage of steel [when)], it is necessary to introduce another resisting couple in the beam. This is done by adding steel in both the compression and tensile sides of the beam.

- Compressive steel increases not only the resisting moments of concrete sections but also the amount of curvature that a member can take before ﬂexural failure. This means that the ductility of such sections will be appreciably increased. Though expensive, compression steel makes beams tough and ductile, enabling them to withstand large moments, deformations, and stress reversals such as might occur during earthquakes. As a result, many building codes for earthquake zones require that certain minimum amounts of compression steel be included in ﬂexural members.

- Compression steel is very effective in reducing long-term deﬂection due to shrinkage and plastic ﬂow.

- Continuous compression bars are also helpful for positioning stirrups (by tying them to the compression bars) and keeping them in place during concrete placement and vibration.

Tests of doubly reinforced concrete beams have shown that even if the compression concrete crushes, the beam may very well not collapse if the compression steel is enclosed by stirrups. If the compression bars are conﬁned by closely spaced stirrups, the bars will not buckle until additional moment is applied.

For doubly reinforced beams, an initial assumption is made that the compression steel yields as well as the tensile steel. (The tensile steel is always assumed to yield because of the ductile requirements of the ACI Code). If the strain at the extreme ﬁber of the compression concrete is assumed to equal 0.003 and the compression steel, A's , is located two-thirds of the distance from the neutral axis to the extreme concrete ﬁber, then the strain in the compression steel equals 2/3 × 0.003 = 0.002. If this is greater than the strain in the steel at yield, as say 420/200000=0.0021 for 420MPa steel, the steel has yielded. It should be noted that actually the creep and shrinkage occurring in the compression concrete help the compression steel to yield.

Sometimes the neutral axis is quite close to the compression steel. As a matter of fact, in some beams with low steel percentages, the neutral axis may be right at the compression steel. For such cases, the addition of compression steel adds little, if any, moment capacity to the beam. It can, however, make the beam more ductile.

When compression steel is used, the nominal resisting moment of the beam is assumed to consist of two parts: the part due to the resistance of the compression concrete and the balancing tensile reinforcing, and the part due to the nominal moment capacity of the compression steel and the balancing amount of the additional tensile steel as illustrated in Figure. In the expressions developed here, the effect of the concrete in compression, which is replaced by the compressive steel, A's, is neglected. This omission will cause us to overestimate Mn by a very small and negligible amount (less than 1%). The ﬁrst of the two resisting moments is illustrated in Figure (b).

The second resisting moment is that produced by the additional tensile and compressive steel (As2 and A's), which is presented in Figure (c).

Up to this point it has been assumed that the compression steel has reached its yield stress. If such is the case, the values of As2 and A's will be equal because the addition to T of As2fy must be equal to the addition to C of A's fy for equilibrium. If the compression steel has not yielded, A's must be larger than As2. Combining the two values, we obtain:

The addition of compression steel only on the compression side of a beam will have little effect on the nominal resisting moment of the section. The lever arm, z, of the internal couple is not affected very much by the presence of the compression steel, and the value of T will remain the same. Thus, the value Mn = Tz will change very little. To increase the nominal resisting moment of a section, it is necessary to add reinforcing on both the tension and the compression sides of the beam, thus providing another resisting moment couple.

In each of these problems, the strain, in the compression steel is checked to determine whether or not it has yielded. With the strain obtained, the compression steel stress fs', is determined, and the value of As2 is computed in the expression:

In addition, it is necessary to compute the strain in the tensile steel, because if it is less than 0.005, the value of the bending, φ, will have to be computed, in as much as it will be less than its usual 0.90 value. The beam may not be used in the unlikely event that  is less than 0.004.

To determine the value of these strains, an equilibrium equation is written compressive strength equal to tensile strength. Only one unknown appears in the equation, and that is c. Initially the stress in the compression steel is assumed to be at yield (f's = fy).  Summing forces horizontally in the force diagram and substituting c for a leads to:

From figure below:

If the strain in the compression steel , the assumption is valid and fs'=E*  is at yield, fy .If  , the compression steel is not yielding, and the value of c calculated above is not correct. A new equilibrium equation must be written that assumes fs' < fy .

and Es=200000MPa

It is highly desirable, that failure, should it occur, by precipitated by tensile yielding rather than crushing of the concrete. This can be ensured by setting an upper limit on the tensile reinforcement ratio. By setting the tensile steel strain in Figure (b) equal to establish the location of the neutral axis for the failure condition and then summing horizontal forces shown in Figure (c) (still assuming the compressive steel to be at the yield stress at failure), it is easily shown that the balanced reinforcement ratio  for a doubly reinforced beam is:

where  is the balanced reinforcement ratio for the corresponding singly reinforced

beam and. The ACI Code limits the net tensile strain, not the reinforcement ratio. To provide the same margin against brittle failure as for singly reinforced beams, the maximum reinforcement ratio should be limited to:

if  then

Because establishes the location of the neutral axis, the limitation will provide acceptable net tensile strains. A check of  is required to determine the strength reduction factor and to verify net tensile strain requirements are satisfied. Substituting  for  in above equation will give the maximum reinforcement ratio for  = 0.90.

The value of c determined enables us to compute the strains in both the compression and tensile steels and thus their stresses.

Ex.8: Find the ultimate moment capacity for the section below, using fy = 345MPa and f 'c=27.6MPa?

As = 4828mm2 and As' =2414mm2   Assume fs = fs’=  fy =345MPa

o.k. under reinforced beam

And     As2*fy  = As' * fy    As2 = As' = 2414mm2

and As1= 4828-2414 =2414mm2

Ex. 9: Compute the design moment strength of the section shown if fy = 420MPa and

F'c =  27.6 MPa.

As =3217 mm2 and As' =760mm2

Assume fs = fs’= fy =420MPa

8

o.k. under reinforced beam

And     As2*fy  = As' * fs'

As1= As – As' = 3217 -602.57 = 2614.43 mm2

.

Ex. 10:  Find the ultimate moment capacity and maximum live load that could be applied for the section of the beam below, using fy= 400 MPa and f 'c =21MPa?

As2=As’=628.6mm2 ,  As =2946 mm2

Assume fs = fs’=  fy =400MPa

4

o.k. under reinforced beam

And     As2 = As'

As1= As – As' = 2946 -628.6 = 2317.4 mm2

Wu= 56.885  kN/m

Wu = 1.2(0.3*0.6*24) + 1.6 WL.L = 56.885   Then     WL = 32.313 kN/m.

3.11.2 Design of doubly reinforced beams:

Sufficient tensile steel can be placed in most beams so that compression steel is not needed. But if it is needed, the design is usually quite straight forward. The design procedure follows the theory used for analyzing doubly reinforced sections.

Ex.11: Design a rectangular beam for MD = 200kN.m and ML = 350kN.m if f'c = 25MPa and fy =420MPa. The maximum permissible beam dimensions are shown in below.

For checking of  there is no economic efficiency of using  Then use

and

For compression reinforcement use bars

For tension reinforcement As= As1 +As2 =  +1668.4 = 4660.52 mm2 use bars

Check solution for actual reinforcement:

The beam is under reinforced and its strength is:

Ex. 12: Find total area of steel required for the section below which supports Mu= 400kN.m , using fy = 420MPa f’c =21MPaand  d’= 65mm if you need compression reinforcement?

Try first as singly reinforced beam with

Comp.  reinf.   required Mn1= 290.38 kN.m

and   Mn2= 400 – 290.38 = 109.62 kN.m

As tension total= 1923.75 + 707.3 = 2631.05 mm2

then

For compression reinforcement use bars

For tension reinforcement As= As1 +As2 =  + 707.3 = 2631.05  mm2 use bars

Check solution for actual reinforcement:

3.12 Analysis and design of T or L beam:

Reinforced concrete ﬂoor systems normally consist of slabs and beams that are placed monolithically. As a result, the two parts act together to resist loads. In effect, the beams have extra widths at their tops, called ﬂanges, and the resulting T-shaped beams are called T-beams. The part of a T beam below the slab is referred to as the web or stem. (The beams may be L shaped if the stem is at the end of a slab.) The stirrups in the webs extend up into the slabs, as perhaps do bent-up bars, with the result that they further make the beams and slabs act together.

There is a problem involved in estimating how much of the slab acts as part of the beam. If, however, the ﬂanges are wide and thin, bending stresses will vary quite a bit across the ﬂange due to shear deformations. The farther a particular part of the slab or ﬂange is away from the stem, the smaller will be its bending stress.

Instead of considering a varying stress distribution across the full width of the ﬂange, the ACI-318-14 Code (6.3.2.1). The objective is to have the same total compression force in the reduced width that actually occurs in the full width with its varying stresses.

The hatched area in Figure above shows the effective size of a T beam. The code states the table below for width of beams with ﬂanges on both sides of the web and one side.

Table 6.3.2.1 Dimensional limits for effective overhanging

flange width for T-beam.

| Flange location | Effective over hanging flange width beyond face of web |
| --- | --- |
| Each side of web | Least of | 8hf |
|  |  | Sw/2 |
|  |  | Ln/8 |
| One side of web | Least of | 6hf |
|  |  | Sw/2 |
|  |  | Ln/12 |

Where Sw =clear span between web, Ln = length of beam.

6.3.2.2 Isolated non-prestressed T-beams in which the flange is used to provide additional compression area shall have a flange thickness greater than or equal to 0.5bw and an effective flange width less than or equal to 4bw.

The analysis of T beams is quite similar to the analysis of rectangular beams in that the speciﬁcations relating to the strains in the reinforcing are identical. To repeat brieﬂy, it is desirable to have  values ≥ 0.005, and they may not be less than 0.004 unless the member is subjected to an axial load ≥ 0.10*f'c* Ag.   values are almost always much larger than 0.005 in T beams because of their very large compression ﬂanges. For such members, the values of c are normally very small, and calculated  values very large.

The neutral axis (N.A.) for T beams can fall either in the ﬂange or in the stem, depending on the proportions of the slabs and stems. If it falls in the ﬂange, and it almost always does for positive moments, the rectangular beam formulas apply, as in Figure (a). The concrete below the neutral axis is assumed to be cracked, and its shape has no effect on the ﬂexural calculations. The section above the neutral axis is rectangular.

If the neutral axis is below the ﬂange, however, as shown for the beam of Figure (b), the compression concrete above the neutral axis no longer consists of a single rectangle, and thus the normal rectangular beam expressions do not apply.

3.12 .1 Analysis of T or L Beams

The calculation of the design strengths of T beams depend on the neutral axis position, if it falls in the ﬂange then is was considered as rectangular sections, while it is T section if the neutral axis is at the web. The procedure used for both cases involves the following steps:

- Check As min as per ACI Section 10.5.1 using bw as the web width.

2. Compute T = As fy .

3. Determine the area of the concrete in compression (Ac) stressed to 0.85f'c

C = T = 0.85f'c* Ac    and

4. Calculate a, c and  .

5. Calculate φMn .

Ex. 13: Determine the design strength of the T beam shown in Figure below, with f'c= 25MPa and fy = 420MPa. The beam has a 10m span and is cast integrally with a ﬂoor slab that is 100mm thick. The clear distance between webs is 1250mm.

≤ 10000/4=2500 mm

≤250+16*100=1850mm

≤1250+250=1500mm             Then use

C = T = 0.85f'c* Ac    and

Flange area = 100*1500 =150000

Ex.10:find the moment section capacity for the isolated  (T) beam shown,using f’c= 20MPa and fy=400MPa. Try  As=4800mm2.

C = T = 0.85f'c* Ac    and

Flange area = 150*720 =108000

Another Method for Analyzing T Beams

First, the value of a is determined, if it is less than the flange thickness, hf , rectangular beam and the rectangular beam formulas will apply. And if it is greater than the flange thickness, hf , then T section.

The beam is divided into a set of rectangular parts consisting of the overhanging parts of the flange and the compression part of the web. The total compression, Cw, in the web rectangle, and the total compression in the overhanging flange, Cf , are computed:

Then the nominal moment, Mn , is determined from compression forces  by multiplying Cw and Cf  by their respective lever arms from their centroid to the centroid of the steel:

Or from force balanced=

And

Then

for value

As for rectangular beams, the tensile steel should yield prior to sudden crushing of the compression concrete, as assumed in the preceding development. Yielding of the tensile reinforcement and Code compliance are ensured if the net tensile strain is greater than 0.004.

From the geometry of the section,

Setting  = 0.003 and  = 0.004 provides a maximum c/dt, ratio of 0.429. Thus, as long as the depth to the neutral axis is less than 0.429 dt , the net tensile strain requirements are satisfied, as they are for rectangular beam sections. This will occur if   is less than:

where   and   as previously defined for a rectangular cross section.

Note : For T or L (ACI-Code - section10.5.2 — For statically determinate members with a flange in tension, As,min shall not be less than the value given by Eq. (10-3)

except that bw is replaced by either 2bw or the width of the flange, whichever is smaller).

Ex.14:  A concrete Slab with 80mm supports on beams the distance between them 1.8m clc with simply supported span of 5m, find ultimate moment capacity for the interior beam, using f’c = 20.7MPa and fy = 345MPa, d=600mm.Use 8  32= 6436 mm2

Solution:

Then use    For As =6434   mm2

then  T-section

for

under reinforced beam.

3.12.2 Design of L and T beams

For the design of T or L beams, the ﬂange has normally already been selected in the slab design, as it is for the slab. The size of the web is normally not selected on the basis of moment requirements but probably is given an area based on shear requirements; that is, a sufficient area is used so as to provide a certain minimum shear capacity. It is also possible that the width of the web may be selected on the basis of the width estimated to be needed to put in the reinforcing bars. Sizes may also have been preselected, to simplify formwork for architectural requirements or for deﬂection reasons.

The ﬂanges of most T beams are usually so large that the neutral axis probably falls within the ﬂange, and thus the rectangular beam formulas apply. Should the neutral axis fall within the web, a trial-and-error process is often used for the design. In this process, a lever arm from the center of gravity of the compression block to the center of gravity of the steel is estimated to equal the larger of 0.9d or (d − (hf/2), and from this value, called z, a trial steel area is calculated (As = Mn /fy z ).

If there is much difference, the estimated value of z is revised and a new As determined. This process is continued until the change in As is quite small.

The bending moment over the support is negative, so the ﬂange is in tension. Also, the magnitude of the negative moment is usually larger than that of the positive moment near mid span. This situation will control the design of the T beam because the depth and web width will be determined for this case. Then, when the beam is designed for positive moment at mid span, the width and depth are already known.

Ex.15:A simply supported beam(TT) shown below supports service dead load of 20kN/m and service live load of 35kN/m using strength design method find steel area required for the beam ,use f’c= 24MPa and fy = 400MPa d= 510 and d’=60mm?

Wd= (0.9*0.6 – 0.45*0.6) *24= 6.48 kN/m

Wu= 1.2*(20+6.48) +1.6*35 =87.67 kN/m

For –ve moment rectangular section= -536.99kN.m

Mu2= 536.99 – 458.1 = 78.89  kN.m

As1= 0.0204*300*510 = 3121.2 mm2

Ast = 3121.2 + 486.98 = 3608.18  mm2

Then  As' = As2 =  mm2

Check:

For T or L (ACI-Code - section10.5.2 — For statically determinate members with a

flange in tension, As,min shall not be less than the value given by Eq. (10-3)

except that bw is replaced by either 2bw or the width of the flange, whichever is smaller).

For +ve moment= 639.58kN.m

Try a = hf = 150mm  try

=     then rectangular section.

Check:

Try using

Ex.16: Find area of steel required for the beams B-1and B-2 for the plan shown, using f’c = 20MPa and fy = 400MPa.

Loads    B-1    B-2

Wd        55      27.5 kN/m (including its own weight)

WL      100     50 kN/m

For interior beam B-1:

Then use

Wu= 1.2 *55 + 1.6 * 100= 226 kN/m

Mu= 226*(5)2/8 = 706.3 kN.m

Try a = hf = 75mm try

then T- section

Muw = 706.3 - 530.8 = 175.5 kN.m

a = 102.2 mm

As-total = 3188 + 1085.9 =  4273.9 mm2

Check

For exterior beam B-2:

Then use

Wu= 1.2 *27.5 + 1.6 * 50= 113 kN/m

Mu= 113*(5)2/8 = 353.13  kN.m

Try a = hf = 75mm

Then rectangular- section

Check

Analysis and design of Irregular sections

Then

اما اذا كان المقطع مثلث ولايحوي اي مستوي يتم مباسرة حساب X بعد حساب  b1) ( من تشابه المثلثات

ثم يتم حساب موقع مركز هذه المساحة

اما لحساب خضوع الحديد فيجب حساب مساحة الحديد Asb  وثم حساب Asmax

Ex.17 : Find the moment section capacity for the beam shown, using f’c = 28MPa and fy = 400 MPa and  As = 2800mm2?

Then

Area of         equal = 0.5*300*150 = 22500mm2

so we must add another area X*b

= 22500+300*X

then X = 81.86 mm   and   a = 150 + 81.86 = 231.86 mm

Calculate

then

Ex.18: Find ultimate section capacity for the section, using f’c =25 MPa and fy =400MPa.

Then

Area of         equal = mm2  so we must add another area X*b

46381.2 = 30000 + 400*X          then X = 40.95 mm   and a = 100+40.95= 140.95 mm

Calculate

Ex. 16: Find area of steel required for the beams shown, using f’c = 28MPa and fy = 400 MPa, the external moment applied is Mu= 450kN.m?

Try a= 150mm

Add part of web: 450-292.38 =157.62 kN.m

157.62*106 = 0.9* 0.85 * 28 [400 * x (530-150-x/2)]

Ast = 3022.6 mm2

Sheet no. 2

Q.1 : Check the adequacy of the beam shown using f’c=34MPa and fy=380MPa?

Q.2: Find maximum load that could be applied on the beam shown , using f’c=30MPa and fy=400MPa and As=2000mm2,the ratio of  live load to dead load =2 (neglect weight of beam)?

Q.3: determine the maximum live load that could be applied if A’s=0.35 As, f’s= 0.89 fy , fy=400MPa and f’c=30MPa. (Neglect weight of beam)?

Q.4: For the section below find ultimate section capacity if As=3800mm2 for the first two ,f’c=25 and fy=380MPa?

Q.5: Design the beam shown, it support dead load (including its own weight ) =10kN/m and one concentrated live load of 30kN. Use f’c=24MPa and fy =380MPa?

Q.6: Find total area of steel required for (positive and negative moment) the beam shown, the material properties are f’c=25MPa and fy= 400Mpa?